12 micron Metallized PET Film

Characters：1.High Brightness 2.Good gas and light barrier. UV transmission rate is below 3.Strong aluminum adhesion. Good barrier of moisture, heat and puncture,Sometimes it can replace aluminum foil

Application：It is widely used for food packaging, industrial packaging, lamination, printing, label, and etc. It is applied in various top grade wine and cigarette packaging, gift boxes, silver and golden cardboards, also applied for milk powder, tea, pharmacy, food and brands.

| NO. | Properties | Unit | Standard Values | Test Method |
| --- | --- | --- | --- | --- |
| 1 | Standard Thickness 标准厚度 | mic | 12 |  |
| 2 | Film Thickness Tolerance 厚度公差 | % | ≦ | 5 | ASTM-D374 |
| 3 | Tensile Strength MD 抗拉强度 TD | Mpa | ≧ | 200 | ASTM-D882 |
|  |  |  | ≧ | 200 |  |
| 4 | Elongation at Break MD 断裂伸长率 TD | % | ≧ | 100 |  |
|  |  |  | ≧ | 100 |  |
| 5 | Heat Shrinkage(150℃/30min) MD 热收缩率 TD | % | ≦ | 1.5 | ASTM-D1204 |
|  |  |  | ≦ | 0.5 |  |
| 6 | Wetting Tension 润湿张力 | mN/m | ≧ | 52 | ASTM-2578 |
| 7 | Vapor Permeation Flux 水蒸汽透过率 | g/m2.24h | ≦ | 3.5 | ASTM-F1249 |
| 8 | Oxygen Permeation Flux 氧气透过率 | cm3/(m2.24h.0.1MPa) | ≦ | 15 | ASTM-F1927 |
| 9 | Strong adhesive strength 附着力 | % | ≦ | 20 | --- |
| 10 | Aluminum-plate thickness 铝层厚度 | Ω/□ | ≧ | 2.0 | --- |
| 11 | Aluminum-plate equality 铝层均匀度 | % | ± | 15 | --- |